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	Content
	Answer

	1
	In order to ensure the flexible of the FPC, we suggest to remove the inner coverlay, Please confirm!
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LAYER DESCRIPTION NOMINAL THICKNESS (um)
COVERLAY POLYIMIDE 12.5 (+/- 1.5)
ADHESTVE: MOD EPOXY 20.0 (+/- 3.0)

COPPER: 1/30Z CU+PLATING 12.0 (+/- 3.0)

BASE: POLYIMDE 20.0 (+/- 2.5)
ADHESIVE: MOD EPOXY 25.0 (+/- 3.0)
COVERLAY: POLYIMIDE 12.0 (+/- 1.5)

ADHES MOD_EPOXY 18.0 (/- 3.0)

COPPER: 1/30Z CU 12.0 (+/- 3.0)

BASE: POLYIMDE po o /-2 5)]e 18um
COPPER: 1/307 CU+PLATING 12.5 (/- 3.0 = 12um
ADHESIVE: MOD EPOXY 20,0 (+/- 3.0)
COVERLAY: POLYIMIDE 12.5 (+/- 1.5)





In the drawing, because there is not point the thickness about the ZIF area or the bottom stiffener on this area, so we can’t build the finally stack-up.so can you please also sent the ZIF spec to us, thanks!
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	Confirmed.
Recommended FPC thickness is 0.20 +/- 0.03 mm, at ZIF connector.

Stiffener = 67.5 UM, or 0.0675mm.

	2
	 We added the pull tap as following drawig.Pls confirm. 
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	Confirmed.

	3
	For the below Item 13, the liner thickness should be 0.1mm, pls revised the drawing.
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	Confirmed.

	4
	We suggest the tolerance about the adhesive 、silk screen and stiffener is +/-0.3mm.  Please confirm!
	Confirmed.

	5
	In order to prevent the FR4 stiffener exceed the outline, we suggest reduce the stiffener 0.1mm smaller on the rectangle area as below, and we will add the silkscreen line per lay up FR4 stiffener. Please confirm!
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	Confirmed.

	Report
	JJ Wang
	Check
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